- Creep

# Concrete Propertie

  - Deformations (strains) under sustained loads.

P

L

L, elastic

L, creep

P

=L/L

Like shrinkage, creep is not completely

- Magnitude of creep strain is a function of all the above that affect shrinkage, plus

  - magnitude of stress

  - age at loading

- Creep strain develops over time…

  - Absorbed water layers tend to become thinner between gel particles that are transmitting compressive stresses

  - Bonds form between gel particles in their deformed position.

where,

Concrete Propertie

- Tri-axial Compression

  - Confined Cylinder

- Example: spiral reinforced

1

1  f 'c  4.1 3

F1 = longitudinal stress at failure F3 = lateral pressure

F

3

F1

Improved strength and ductility versus uniaxial compression	F

# concrete Propertie

- Tri-axial Compression

Fig. 3-15, MacGregor (1997)

# Steel Reinforcement

  - General

–	Standard Reinforcing Bar Markings

    - General

# Steel Reinforcement

      - Most common types for non-prestressed members:

        - hot-rolled deformed bars

        - welded wire fabric

# Steel Reinforcement

      - Areas, Weights, Dimensions

# Steel Reinforcemen

    - Types

      - ASTM A615 - Standard Specification for Deformed and Plain-Billet Steel Bars

        - Grade 60: fy = 60 ksi, #3 to #18

          - most common in buildings and bridges

        - Grade 40: fy = 40 ksi, #3 to #6

          - most ductile

        - Grade 75: fy = 75 ksi, #6 to #18

# Steel Reinforcement

- Types

  - ASTM A616 - Rail-Steel Bars

  - ASTM A617 - Axle-Steel Bars

  - ASTM A706 - Low-Alloy-Steel Bars

    - more ductile GR60 steel

    - min. length of yield plateau = sh/y = 5

# Steel Reinforcement

- Stress versus Strain

– Stress-Strain curve for various types of steel reinforcement bar.

# Steel Reinforcemen

- Es = Initial tangent modulus

= 29,000 ksi (all grades)

Stress

- Note:	Es

GR40 has a longer	1

yield plateau

GR 60 (less ductile) GR 40

0.20

S